## Slide 1
SiO2, d = 815 nm
Ta2O5, d = 458 nm
SiO2, d = 663 nm
Ta2O5, d = 457 nm
SiO2, d = 673 nm
Ta2O5, d = 457 nm
SiO2, d = 668 nm
Ta2O5, d = 460 nm
SiO2, d = 669 nm
Ta2O5, d = 455 nm
SiO2, d = 669 nm
Ta2O5, d = 465 nm
SiO2, d = 670 nm
Ta2O5, d = 460 nm
SiO2, d = 532 nm
Plot of useful solar power transmitted through the structure compared to total useful solar power assuming ; i.e. the red curve is where is the transmission spectrum of the multilayer
Plot of solar power transmitted through the structure between 750 nm and 3200 nm; i.e. the red curve is where is the transmission spectrum of the multilayer

## Slide 2
SiO2, d = 815 nm
Ta2O5, d = 458 nm
SiO2, d = 663 nm
Ta2O5, d = 457 nm
SiO2, d = 673 nm
Ta2O5, d = 457 nm
SiO2, d = 668 nm
Ta2O5, d = 460 nm
SiO2, d = 669 nm
Ta2O5, d = 455 nm
SiO2, d = 669 nm
Ta2O5, d = 465 nm
SiO2, d = 670 nm
Ta2O5, d = 460 nm
SiO2, d = 532 nm
Plot of trapped thermal radiation from the multilayer structure compare to total thermal radiation of a blackbody at 440 K, i.e. plot of where is the reflectance spectrum of the multilayer stack
Optimized Multilayer